Supplementary material

Tailoring Hydrophobicity: Synthesis, Characterization and Application of Pyridinium-based Surfactants as Corrosion Inhibitors

Maham Almas1*, Rabia Talat 1,2*, Ubaid Ullah Khan3*, Saira Fatima1, Ali Haider 1,4*, Syed Mustansar Abbas5, Saqib Ali1

1Department of Chemistry, Quaid-i-Azam University, Islamabad 45320, Pakistan.

2Department of Chemistry, Rawalpindi Women University, Satellite Town, 6th Road, Rawalpindi, Pakistan.

3Department of Chemical Sciences, University of Lakki Marwat, KPK, Pakistan

4Pakistan Academy of Sciences, 3 Constitution Ave, G-5/2 Islamabad, Pakistan.

5Nanoscience and Technology Department, National Center for Physics, Quaid-i-Azam    University Campus, Islamabad, Pakistan.

*Corresponding Author: Ali Haider (ahaider@qau.edu.pk ); Ubaid Ullah Khan (ubaidullahkha0307@gmail.com ); Maham Almas (malmas@chem.qau.edu.pk ); Rabia Talat (rabiatalat@chem.qua.edu.pk )

Supplementary material

Table S1. Chemical composition of CR4 mild steel.

| Element | C | Mn | Si | P | Al | Fe |
| --- | --- | --- | --- | --- | --- | --- |
| Chemical composition (weight %) | 0.12 | 0.60 | 0.45 | 0.04 | 0.02 | Balance |

FT-IR and NMR Spectroscopy Data

a) n-Octyl-2-methylpyridinium bromide (MP8)

Brown Viscous Liquid, Yield (92.1%), 1H NMR (300MHz, CDCl3, δ-ppm): 8.42 (1H, H2, d), 7.91 (1H, H3, t), 8.36 (1H, H4, t), 9.34 (1H, H5, d), 2.94 (3H, H6, s), 4.70 (2H, H7, t), 1.1-1.87 (12H, H8-13, m), 0.79 (3H, H14, t). 13C NMR (75.5 MHz, CDCl3, δ-ppm): 154.2 (C1), 126.4 (C2), 146.1 (C3), 130.4 (C4), 147.3 (C5), 20.6 (C6), 58.3 (C7), 22.4-31.5 (C8-C13), 13.9 (C14). FT-IR (υ cm-1); 1300 (C-N), 1630 (C=N), 1575 (C=C), 1464 (-CH2), 3039(CH-Aromatic), 1141 (-CH3).

b) n-Decyl-2-methylpyridinium bromide (MP10)

Brown viscous liquid, Yield (98.5%)1H NMR (300 MHz, CDCl3, δ-ppm): 8.41 (1H, H2, d), 7.93 (1H, H3, t), 8.38 (1H, H4, t), 9.39 (1H, H5, d), 2.92 (3H, H6, s), 4.74 (2H, H7, t), 1.1-1.92 (16H, H8-15, m), 0.83 (3H, H16, t). 13C NMR (75.5 MHz, CDCl3, δ-ppm): 154.2 (C1), 126.4 (C2), 146.3 (C3), 130.4 (C4), 145.3 (C5), 20.73 (C6), 58.4 (C7), 22.5-31.7 (C8-C15) 14.07 (C16). FT-IR (υ cm-1); 1300 (C-N), 1630 (C=N), 1574 (C=C), 1465 (-CH2), 3048 (CH-Aromatic), 1141 (-CH3).

c) n-dodecyl-2-methylpyridinium bromide (MP12)

Light Brown solid, Yield (80.7%), MP (54-56οC) 1H NMR (300 MHz, CDCl3, δ -ppm):8.41 (1H, H2, d), 7.95 (1H, H3, t), 8.39 (1H, H4, t), 9.38 (1H, H5, d), 2.90 (3H, H6, s), 4.75 (2H, H7, t), 1.2-1.98 (20H, H8-17, m), 0.82 (3H, H18, t). 13C NMR (75.5 MHz, CDCl3, δ-ppm): 154.2 (C1), 126.4 (C2), 146.3 (C3), 130.4 (C4), 145.3 (C5), 20.74 (C6), 58.4(C7), 22.65-34.0 (C8-C17), 14.0 (C18). FT-IR (υ cm-1); 1307 (C-N), 1629 (C=N), 1573 (C=C), 1462 (-CH2), 3043 (CH-Aromatic), 1170 (-CH3).